SPECIFICATION

Sections 07 90 00 / 07 95 00

(Formerly sections 05810 / 07102 / 07915)

LokCrete Membrane System

LMS Series

Waterproof Expansion Joint Sealing System

# PART 1 – GENERAL

  - Work Included

- The work shall consist of furnishing and installing waterproof expansion joints in accordance with the details shown on the plans and the requirements of the specifications.  The expansion joints utilize extruded elastoprene seals combined with elastomeric concrete headers.

- Related Work

- Section 03300 - Cast-in-place concrete

- Section 05500 - Miscellaneous metal / expansion joints

- Section 07600 - Flashing and sheet metal

- Section 07900 - Sealants, caulking and waterproofing

  - Submittals

- General – Submit the following according to Division 1 Specification Section.

- Standard Drawings – Submit typical expansion joint drawings indicating pertinent dimensions, general construction, blockout dimensions and product information.

  - Product Delivery, Storage and Handling

- Deliver products to site in Manufacturer’s original, intact, labeled containers and store under cover in a dry location until installed.  Store off the ground in temperatures above 40ºF, protect from weather and construction activities.

  - Basis of Design

- All joints shall be designed to meet the specified performance criteria of the project as manufactured by MM Systems Corp., 50 MM Way, Pendergrass, GA, 30567. Tel. 866.506.6929 Fax. 706.824.7501 Web.  www.mmsystemscorp.com

- Alternate manufacturers will not be considered for this project due to insufficient product evaluation time. Submit for future evaluation, products that meet the design criteria and exhibit performance features that are equal to or superior to those called for in the base product specification. Submittal of alternates must be made two weeks prior to bid opening on future projects to allow proper evaluation time. Alternate products not adhering to all listed design features will not be considered. Final decision will be at the sole discretion of the architect or consulting engineer.

## Quality Assurance

- Pre-construction – the General Contractor, Engineer/Architect, Concrete Subcontractor, Manufacturer’s Representative and Certified Contractor, will conduct a pre-construction meeting to discuss blockout construction, joint gap settings and construction phasing. This meeting shall be held prior to any concrete placement at expansion joint blockouts and may be held in conjunction with the concrete pre-pour meeting.

- Joint Opening Adjustment – the Project Engineer shall provide calculations to the concrete subcontractor to adjust the nominal joint opening the day of the concrete placement. Use a “temperature adjustment table” with expansion joint openings calculated in five (5ºF) degree increments based on a temperature range of [adjust for project] -20ºF to 120ºF. Expansion joints shall not be installed until the structure has undergone its anticipated short-term shortening and creep.

- Expansion Joint Blockouts - shall be floated and troweled before final cure to remove all air pockets, voids and spalls caused by formwork.

- Areas Adjacent to Expansion Joint - two feet on each side of joint gap shall be finished and graded perpendicular to joint gap creating flush slab-to-slab transition with identical elevations. Creation of an elevated concrete wash is recommended at these locations to insure a downward slope for water drainage.

- Pre-installation Inspection – the General Contractor, Engineer/Architect, Manufacturer’s Representative and Certified Contractor, will conduct a pre-installation project site inspection. The General Contractor shall provide a field report that summarizes the project conditions and any remedial action necessary to correct field conditions (substrate, joint size, blockout, vertical offsets, etc.) that may affect expansion joint system performance.

- Service Condition - insure that anticipated service conditions (loads, speed of traffic, movement, etc) are part of the expansion joint system selection criteria.

- Certification / Installation – a factory-trained and “certified” contractor shall install the specified expansion joint system. Proof of certification from manufacturer and proof of participation in manufacturer’s continuing education program is required.

- Warranty – the Manufacturer and Certified Contractor jointly warrant to the Owner that the expansion joint system shall be free from manufacturing, material and installation defects for a period of five (5) years from the date of installation, based on specified movements and design conditions for normal traffic use as recommended by the National Parking Association’s “Parking Facility Maintenance Manual” and subject to the terms and conditions of the manufacturer’s standard written limited warranty. The warranty covers leakage at the joint under normal use due to cohesive or adhesive failure and material failure related to tearing, weathering or abrasion.  No liability or responsibility is accepted due to defects in the concrete. The Certified Contractor and Manufacturer will jointly warrant and provide at no charge, all materials and labor needed to properly repair defective expansion joint within the term of the warranty.

## PART 2 – PRODUCT

  - General

- Provide watertight expansion joint sealing system that meets the specified movement requirements and is capable of accommodating vehicular and pedestrian traffic.

- System shall consist of elastoprene rubber seals with integral wing side flanges that are secured to the concrete deck using an elastomeric concrete header. Elastomeric concrete headers requiring primers to bond to the concrete will not be allowed. The rubber seal must include tire impact dampening bulkhead design and microsealant waterproofing under the wings of the seal. Slab to wall conditions require a seal design specific to that application – turning up the side flange is not permissible.

- Furnish approved LokCrete Membrane System “LMS Series” as manufactured by MM Systems Corporation.

- Select the system size at each joint location based on the movement and design requirements that meet the project specification or as defined by the structural engineer of record.

- The Certified Contractor must provide written confirmation; utilizing manufacturer’s product data confirming that the membrane seal selected will comply with and accommodate expansion, contraction and lateral shear throughout the full movement cycle.

  - Components and Materials

- Membrane Seal – Material shall be a flexible, extruded thermoplastic elastoprene rubber compound exhibiting the physical properties listed in the table below.  The seal design shall have factory-punched holes in the wing flaps through which the elastomeric concrete header material bonds the seal to the deck to ensure watertightness and proper joint performance.

Elastoprene membrane seal must exhibit the following physical properties.

Property			         Requirement	         ASTM Method

Tensile Strength		     	1000 psi (+75/-0)	D412

Ultimate Elongation			445%			D412

Hardness, Shore A			65 +/- 3 pts.		D2240

Tear Strength		140 pli / 24.5 kN/m @ 23(C		D624

58 pli / 10.2 kN/m @100(C		D624

Compression set

168 hrs.			25% @ 23(C		D395

168 hrs.			38% @ 100(C		D395

Ozone Resistance			No Cracks		D1149

UV Resistance			Very Good

Brittle Point				-76(F(-60(C)		D746

- Elastomeric Concrete – provide LokCrete( elastomeric concrete header material as manufactured by MM Systems Corporation. Elastomeric concrete shall be produced in an ISO2001 manufacturing facility consisting of polyurethane liquid components “A” and “B” and a specialty aggregate component “C”.  Elastomeric concrete must cure exothermically.

Physical Properties of Elastomeric concrete binder after seven-day cure at room temperature:

##### Property				Requirement	           ASTM Method

Tensile Strength			4750 psi		D412

Compressive strength			9200 psi 		D695

Ultimate Elongation			10% 			D412

Hardness, Shore D			78 +/- 5		D2240

Tear Resistance			200 pli / 35 kN/m	D624

Water Absorption			3%			D570

Heat Shrinkage, max.			2%			D1299

Compression Set			48%			D395

Pot Life				25 minutes 		(after mixing)

Physical Properties of Elastomeric concrete binder & aggregate mix:

##### Physical Property			Requirement             	ASTM Method

Compressive strength			2800 psi 		D695

Resilience @ 5% deflection		95%			D695

Compressive stress, psi		800 psi min.		D695

Impact resistance, ft-lb, @ -20(F	No Cracks		Ball drop

Adhesion				Concrete Failure	D421

- Rubber Polymer Activator – provide manufacturer’s single component liquid chemical activator that allows polymers of the rubber seal and the elastomeric concrete to chemically cross-link.

  - Life Safety – Fire Barrier Systems (as required)

- Approved PyroFlex( Fire Barrier Systems (UPF Series), as manufactured by   MM Systems Corporation - Supply fire-resistive barrier systems that have ratings equal to or greater than the rating of adjacent construction when tested in accordance with ASTM E1966 and UL2079. Provide specified (2, 3 or 4 hour) rated fire barrier expansion joint assembly.

- Fire Barrier System shall be capable of anticipated movement and maintain fire rating through precondition cycling and fire performance testing. System shall have factory and field-tested splices.  Manufacturer shall provide field-splicing instructions.

- Fire Barrier System shall have been tested in accordance with ASTM E1966 and UL2079 at a maximum joint opening as defined by ASTM E1399 that meets or exceeds the maximum joint opening required by the project design requirements. System and manufacturer shall be listed with an accredited independent laboratory.

  - Fabrication

- Elastoprene Membrane Seal – Ship in the longest practical continuous length coiled on manufacturer’s standard reel or on wooden pallets and shrink-wrapped.

- Membrane Seal Mitered Directional Changes – provide factory pre-fabricated directional changes for 90( corners, tees and crosses.

Only straight butt splice connections shall be spliced on the jobsite. Utilize steel splice reinforcing pins and chemically weld with Elastoprene Splice Adhesive. Insure that all internal and external webs of the seal profile are properly bonded at all splice locations.

- Elastomeric Concrete Header – Ship in manufacturer’s approved containers shrink wrapped on wooden pallets.

- Wall Mount Plate (slab-to-wall condition) – aluminum retainer shall be shipped in standard 10 ft. lengths and shall be cut to length on jobsite where required.

- Fire Barriers (if required) – Ship manufacturer’s standard assembly for the required hourly rating with ends prepared for field splicing.  Assemblies shall be miter cut in the field to accommodate changes in direction.

  - Finishes

- Elastoprene membrane seals shall be supplied in standard black or custom gray colors.

- Elastomeric Concrete Header material shall be supplied in standard black or custom gray colors.

## PART 3 – EXECUTION

  - Installation

- Preparation of the Work Area

- The contractor shall provide properly formed concrete blockouts and expansion joint openings constructed to the exact dimensions and elevations shown on manufacturer’s standard system drawings or as shown on the contract drawings. Deviations from these dimensions will not be allowed without the written consent of the engineer of record.

- The contractor shall clean the concrete blockout of all contaminants by sandblasting immediately prior to installation of expansion joint system.  Concrete form release agents, water repellents, laitance, surface dirt, rust, old sealants and other surface treatments and protective coatings must be removed from the blockout substrate surface in order to obtain the proper elastomeric concrete bond.

- Actual field conditions of existing expansion joint blockouts may be deeper and wider than the proposed new expansion joint system as detailed on the contract drawings. When existing blockout is larger additional elastomeric concrete material shall be used. Do not use an unapproved patching material to fill and reduce blockout depth. When blockout size is smaller it shall be made larger by saw cutting.

- For new construction and full concrete restorations it is recommended to create an elevated concrete wash with a two-foot flat surface at the top. Elevations at the top of the wash shall be above those of the finished deck insuring a downward slope for water drainage.

- For projects without elevated washes it is recommended that the finished concrete slab elevation be identical for a two-foot transition area on each side of the expansion joint opening.

- Mask adjacent concrete surfaces with tape to provide neat, clean joint line, workmanlike appearance.  (Remove tape prior to the curing process)

- Do not install expansion joint systems until the concrete has been air-dried at temperatures at or above 45 degrees F. for at least 28 days minimum and the concrete must have a measured moisture content that is below 4 percent. The blockout area must be completely dry prior to placement of the elastomeric concrete.  Blockouts requiring the use of structural repair materials must be cured for 72 hours.  Blow out the area thoroughly using compressed air.

- The base of the recess must be formed level and at the same elevation across the joint.  The joint sidewall interfaces must be parallel, and continuously equidistant from each other. They are to be perpendicular to the base surfaces of the blockout – making the corner a perfect 90( angle. Any edge or area in need of repair shall utilize structural concrete repair materials.

- Seal and Elastomeric Concrete Header Installation

- The membrane seal element shall be unpackaged and laid in a relaxed position to relieve any temporary coiling from shipment packaging.   Prior to placement, the winged flaps of the membrane seal shall be wiped with an acceptable non-petroleum solvent cleaner such as Denatured Alcohol.

- Refer to Manufacturers Installation Guide for detailed step-by-step instructions on how to install the membrane seal, ElastoBond rubber polymer activator and LokCrete elastomeric concrete header materials.

- IMPORTANT - Premature exposure to vehicular traffic can cause stress on the bond line related to vertical slab deflection. For best results wait a minimum of 24 hours (depending on temperature and humidity) before allowing vehicular traffic to drive over the system (contact manufacturer if faster opening time is required).

  - Clean and Protect

- Protect the system and its components during construction.  Heavy construction vehicles will not be permitted to cross the expansion joint. Subsequent damage to the expansion joint system will be repaired at the general contractor’s expense. After work is complete, clean exposed surfaces with a suitable cleaner that will not harm or attack the finish.

END OF SECTION