SPECIFICATION

Sections 07 90 00 / 07 95 00

(Formerly sections 05810 / 07102 / 07915)

Silicone Self-expanding Impregnated Foam Sealing System

ColorJoint SIF Series

(Waterproof Vertical Expansion Joint Sealing System)

# PART 1 – GENERAL

  - Work Included

- The work shall consist of furnishing and installing waterproof expansion joints in accordance with the details shown on the plans and the requirements of the specifications.  The expansion joints utilize factory applied silicone face seal and a secondary microcell foam impregnated with an acrylic polymer that is UV stable, flame resistant, chemical resistant, and meets ASTM 283, ASTM 518, and DIN 18542.

- Related Work

- Division 3 - Section - Cast-in-place concrete

- Division 4 - Masonry

- Division 7 - Thermal & Moisture Protection

- Division 7 - Sealants, caulking and waterproofing

  - Submittals

- General – Submit the following according to Division 1 Specification Section.

- Standard Submittal Package – Submit typical expansion joint drawings(s) indicating pertinent dimensions, general construction, expansion joint opening dimensions and product information.

  - Product Delivery, Storage and Handling

- Deliver products to site in Manufacturer’s original, intact, labeled containers and store indoors in a dry location until installed.  Store off the ground in temperatures above 40ºF, protect from weather and construction activities.

  - Basis of Design

- All joints shall be designed to meet the specified performance criteria of the project as manufactured by MM Systems Corp., 50 MM Way, Pendergrass, GA, 30567. / Tel. 866.506.6929 / Fax. 706.824.7501 Web. www.mm-usa.com

- Alternate manufacturers will not be considered for this project due to insufficient product evaluation time. Submit for future evaluation, products that meet the design criteria and exhibit performance features that are equal to or superior to those called for in the base product specification. Submittal of alternates must be made two weeks prior to bid opening on future projects to allow proper evaluation time.

## Quality Assurance

- Pre-construction Meeting – the General Contractor, Engineer/Architect, Concrete Subcontractor, Manufacturer’s Representative and Certified Contractor, will conduct a pre-construction meeting to discuss joint gap construction, joint gap settings and construction phasing.

- Joint Opening Adjustment – the Project Engineer shall provide calculations to the concrete subcontractor to adjust the nominal joint opening the day of the concrete placement. Use a “temperature adjustment table” with expansion joint openings calculated in five (5ºF) degree increments based on a temperature range of [adjust for project] -20ºF to 120ºF.

- Pre-installation Inspection – the General Contractor, Engineer/Architect, Manufacturer’s Representative and Certified Contractor, will conduct a pre-installation project site inspection. The General Contractor shall provide a field report that summarizes the project conditions and any remedial action necessary to correct field conditions (substrate, joint size, non-parallel sidewalls, vertical offsets, etc.) that may affect expansion joint system performance.

- Certified Installation – a factory-trained and “certified” contractor shall install the specified expansion joint system. The contractor shall provide proof of certification from manufacturer and proof of participation in manufacturer’s continuing education program.

- Warranty – The expansion joint system, when installed by the Manufacturer’s Certified Contractor, shall be warranted for a period of two (2) years under specified movements and design conditions for vertical and horizontal applications. The warranty covers leakage at the joint under normal use due to cohesive or adhesive failure and material failure related to tearing, weathering or abrasion.  No liability or responsibility is accepted due to defects in the surrounding substrate. The Certified Contractor and Manufacturer will jointly warrant and provide at no charge, all materials and labor needed to properly repair or replace defective product within the term of the warranty.

## PART 2 – PRODUCT

  - General

- Provide watertight silicone expansion joint sealing system that meets the specified movement requirements for structural expansion joints, panel joints, window perimeter joints, EIFS panel joints, curtain walls joints or other penetrations of the building envelope.

- System shall consist of a high performance engineered silicone bellows style seal that is factory applied to a microcell foam seal that is impregnated with an acrylic polymer thereby creating a binary sealing system. The system is factory pre-compressed and then released in the field to expand and fill the expansion joint opening. Color selection must be approved by owner prior to material order placement.

- Furnish approved Silicone Self-expanding Impregnated Foam Sealing System “ColorJoint SIF Series” as manufactured by MM Systems Corporation.

- Select the system size at each joint location based on the movement and design requirements that meet the project specification or as defined by the structural engineer of record. Insure that the anticipated service condition is part of the expansion joint system selection criteria. A minimum of 50% expansion and 50% contraction (compression) is required.

- The Certified Contractor must provide written confirmation; utilizing manufacturer’s product data, insuring the silicone seal selected will comply with and accommodate expansion, contraction and lateral shear throughout the full movement cycle.

  - Components and Materials

- Primary Silicone Bellows Seal – provide ColorJoint SIF Series consisting of a primary flexible, preformed silicone rubber compound exhibiting the physical properties listed in the table below.

### PHYSICAL PROPERTIES OF SILICONE SEAL

(after 14 days at 77(F (25(C) and 50% relative humidity)

Property			            Requirement	         	     ASTM Method

Hardness, Shore A			15 points			C661

Tensile strength @ max.		100 psi (.07 kg/mm2)		D412

Tensile at 25% extension		15 psi (.010 kg/mm2)		C1135

Tensile at 50% extension		20 psi (.015 kg/mm2)		C1135

Peel Strength				25 lb/in (4.46 kg/cm)		C794

Cyclical Movement			+100 / -50%			C719

Staining				None

- Secondary Expanding Impregnated Foam Seal - shall be a micro-cell polyurethane foam impregnated with an acrylic polymer that is UV stable, flame resistant, chemical resistant, and meets ASTM 283, ASTM 518, and DIN 18542.

### PHYSICAL PROPERTIES OF EXPANDING IMPREGNATED FOAM

Property			            Requirement	         	     ASTM Method

Density Average	10 lbs./cu.ft. (160kg/m3)

Resistance – thermal  	3.3 hr. oF-ft2/BTU

Conductivity – thermal	0.05 W/m. oC			C3574

Temp. Stability Range	-39 oF to 186 oF

Shear Strength	8 N/cm2 minimum

Tensile Strength - minimum	21 psi				D3574

Compression Set Resistance	2.5% maximum		D3574

Bleeding (212°F at 20% compress)	No Bleeding

Mildew Resistance	Excellent

Staining	None

Flammability	Self Extinguishing		UL94VO

Flame Spread	Zero 				E84

Flash Point	590 oF (310 oC)

  - Life Safety – Fire Barrier Systems (as required)

- Approved PyroFlex( Fire Barrier Systems (PF or UPF Series), as manufactured by        MM Systems Corporation - Supply fire-resistive barrier systems that have ratings equal to or greater than the rating of adjacent construction when tested in accordance with ASTM E1966 and UL2079. Provide specified (2, 3 or 4 hour) rated fire barrier expansion joint assembly.

- Fire Barrier System shall be capable of anticipated movement and maintain fire rating through precondition cycling and fire performance testing. System shall have factory and field-tested splices.  Manufacturer shall provide field-splicing instructions.

- Fire Barrier System shall have been tested in accordance with ASTM E1966 and UL2079 at a maximum joint opening as defined by ASTM E1399 that meets or exceeds the maximum joint opening required by the project design requirements. System and manufacturer shall be listed with an accredited independent laboratory.

  - Fabrication

- ColorJoint SIF Silicone Seal – supplied in five foot factory pre-compressed standard lengths shipped in manufacturer’s standard packaging.

- Directional Changes – follow manufactures detailed instructions for field splicing.

- Fire Barriers (if required) – Ship manufacturer’s standard assembly for the required hourly rating with ends prepared for field splicing.  Assemblies shall be miter cut in the field to accommodate changes in direction.

  - Finishes

- Silicone seal color shall be selected and approved by the owner from the manufacturer’s standard colors or project specific custom color matching process.

## PART 3 – EXECUTION

  - Installation

- Preparation of the Work Area

- The contractor shall provide a properly formed and prepared expansion joint openings constructed to the exact dimensions and elevations shown on manufacturer’s standard system drawings or as shown on the contract drawings. Deviations from these dimensions will not be allowed without the written consent of the engineer of record.

- The contractor shall clean the joint opening of all contaminants immediately prior to installation of expansion joint system.  Concrete form release agents, water repellents, laitance, surface dirt, rust, old sealants and other surface treatments and protective coatings must be removed from the joint opening sidewalls in order to obtain the proper adhesion.

- The ColorJoint is wider than the joint opening. Release the wrap from around the SIF and allow it to self-expand filling the opening. One side of the SIF has pressure sensitive tape allowing it to adhere to one sidewall of the expansion joint opening. Use wood shims to brace the SIF Seal until it fully expands, at which point they can be removed.

- Seal sizes 5 inches and larger require epoxy sidewall adhesive applied in an intermittent pattern to support the weight of the seal.

- Recess the highest point of the silicone seal 1/4" [5mm] below the wall surface.

- As necessary, mask areas adjacent to the joint with tape to assure neat, clean joint lines.  (Remove tape prior to the curing process.)

- Inject silicone sealant between the seal and joint opening sidewall interface. If necessary due to wall surface irregularities, apply a fillet bead of silicone sealant on each side of silicone bellows surface seal with manufacturer’s silicone. Fill in any voids between the seal and the substrate to insure firm contact and secure bond. Tool immediately to insure firm contact and secure bond.

- Refer to Manufacturers Installation Guide for detailed step-by-step instructions.

  - Clean and Protect

- Protect the system and its components during construction. Subsequent damage to the expansion joint system will be repaired at the general contractor’s expense. After work is complete, clean exposed surfaces with a suitable cleaner that will not harm or attack the finish.

END OF SECTION